SOLDER PROPERTIES

| BS EN29453 Alloy No. | Composition | Melting Range° C | Supersedes BS219 | ISO 9453:2014 |
| --- | --- | --- | --- | --- |
| 1a | Sn63-Pb37 | 183 | Exceeds AP | Alloy No. 101 |
| 2a | Sn60-Pb40 | 183-190 | Exceeds KP | Alloy No. 103 |
| 3 | Sn50-Pb50 | 183-215 | Exceeds F | Alloy No. 111 |
| 1 | Sn63/Pb37 | 183 | A | Alloy No. 102 |
| 2 | Sn60-Pb40 | 183-190 | KP | Alloy No. 103 |
| 3 | Sn50-Pb50 | 183-215 | F | Alloy No. 112 |
| 4 | Sn45-Pb55 | 183-226 | R | Alloy No. 113 |
| 5 | Sn40-Pb60 | 183-235 | G | Alloy No. 114 |
| 6 | Sn35-Pb65 | 183-245 | H | Alloy No. 115 |
| 7 | Sn30-Pb70 | 183-255 | J | Alloy No. 116 |
| 8 | Sn10-Pb90 | 268-302 | – | Alloy No. 122 |
| 9 | Sn8-Pb92 | 280-305 | – | High Temperature |
| 10 | Sn/Pb | 320-325 | – | High Temperature |
| 11 | Sn/Pb/Sb | 183 | - | Electrical |
| 12 | Sn/Pb/Sb | 183-190 | - | Elecrical/Tinning |
| 13 | Sn/Pb/Sb | 183-216 | - | Tinning |
| 14 | Sn39.5-Pb58.2-Sb2.2 | 185-231 | C | Alloy No. 134 |
| 15 | Sn/Pb/Sb | 185-250 | D & L | Plumbing/Jointing |
| 16 | Sn/Pb/Sb | 185-263 | – | Industrial |
| 17 | Sn/Pb/Sb | 185-270 | N | Automotive |
| 18 | Sn95-Sb5 | 230-240 | 95A | Alloy No. 201 |
| 19 | Sn/Pb/Bi | 180-185 | – | Special Applications |
| 20 | Sn/Pb/Bi | 178-205 | – | Special Applications |
| 21 | Sn/Bi | 138 | – | Pb/Cd Free Low Temperature |
| 22 | Sn/Pb/Cd | 145 | T | Low Temperature |
| 23 | Sn/Cu | 230-240 | 99C | Alloy No. 401 |
| 24 | Sn97/Cu3 | 230-250 | 97C | Alloy No. 402 |
| 25 | Sn/Pb/Cu | 183-190 | – | Special Electronic/Electrical |
| 26 | Sn/Pb/Cu | 183-215 | – | Electrical/Industrial |
| 27 | Sn/In | 117-125 | – | Glass to Metal |
| 28 | Sn96/Ag4 | 221 | 96S | Alloy No. 701 |
| 29 | Sn97Ag3 | 221-230 | 97S | Lead Free |
| 30 | Sn62-Pb36-Ag2 | 178-190 | 62S | Alloy No. 171 |
| 31 | Sn/Pb/Ag | 178-180 | – | Special SM Electronics |
| 32 | Pb97.5-Ag2.5 | 304-305 | – | Alloy No. 181 |
| 33 | Pb95-Ag5 | 304-365 | – | Alloy No. 182 |
| 34 | Sn5-Pb93.5-Ag1.5 | 296-301 | 5S | Alloy No. 191 |

Info from:	http://www.billshorthousemetals.co.uk/solder-bars-sticks-and-pellets.htm